## Slide 1: Studying the mechanism behind orbital memory switching in Co/BP
Nikhil Seeja Sivakumar, Sebastian Scherb, Hermann Osterhage, Kira Junghans, Nadine Hauptmann, Alexander Khajetoorians

## Slide 2
Is the mechanism of orbital memory related to local buckling of BP lattice?
Questions:

## Slide 3
Is the mechanism of orbital memory related to local buckling of BP lattice?
Can we quantify adsorption height differences of different states?
Questions:
e-
BP
d?

## Slide 4
Is the mechanism of orbital memory related to local buckling of BP lattice?
Can we quantify adsorption height differences of different states?
Can we quantify the spatial distribution of charge on a semiconductor?
  For Co/BP is the spatial anisotropy in switching related to this?
Questions:
e-
e-
e-
e-
e-
e-
semiconductor
weak dielectric
more hopping
charge delocalized
Many body problem
d?

## Slide 5
Is the mechanism of orbital memory related to local buckling of BP lattice?
Can we quantify adsorption height differences of different states?
Can we quantify the spatial distribution of charge on a semiconductor?
  For Co/BP is the spatial anisotropy in switching related to this?
  Is this a polaron?
Questions:
e-
e-
e-
e-
e-
e-
semiconductor
weak dielectric
more hopping
charge delocalized
Many body problem
d?

## Slide 6
Charging peak
Dip corresponding to the charging peak.
The 3d Co state does not show a clear signature in df.
3d Co state
Fish: Voltage dependent df and dI/dV
16 datasets with 9 different tips.

## Slide 7
Identifying different parabolas
Cannot fit two different parabolas reliably.
Might not have two different LCPD max.
Fitting full range
Fitting individual region

## Slide 8
Voltage dependent df and dI/dV at different heights
Feature around -0.6mV.
  I cross-talk ?
  features in excitation
Dip and peaks shift correspondingly.
(independent of the oscillation)
16 datasets with 9 different tips.
SAMPLE

## Slide 9
-400mV,10pA
Spatial dependence
4 datatsets with 3 different tips.
B
Dip shifts to larger energies away from the atoms
Dip becomes shallow and broader in energy away from the atom

## Slide 10
Spatial extent of charging: charging ring
Current
+550mV
+650mV
Current: disc
df: ring
In frequency shift:
Shape of the ring: isotropic
Contrast within ring: anisotropic
Tip shape?
sample tilt?
Frequency shift
3 datatsets with 3 different tips.
But not all are circular features (tip shape?).

## Slide 11
Spatial extent of charging: charging ring
Current
+550mV
+650mV
Current: disc
df: ring
In frequency shift:
Shape of the ring: isotropic
Contrast within ring: anisotropic
Tip shape?
sample tilt?
Frequency shift
3 datatsets with 3 different tips.
But not all are circular features (tip shape?).

## Slide 12
550mV
650mV
750mV
Coupled atoms: charging ring
Current
Frequency shift
Images and spectra stabilised on top of atom @ -800mV,60pA; -40pm closer
One charging ring for each fish.
With increasing voltage, charging ring expands. (Looks like it crosses each other)
The crossed ring part has darker contrast.
On top right & top left there is a butterfly

## Slide 13
550mV
650mV
750mV
Coupled atoms: charging ring
Current
Frequency shift
Images and spectra stabilised on top of atom @ -800mV,60pA; -40pm closer
One charging ring for each fish.
With increasing voltage, charging ring expands. (Looks like it crosses each other)
The crossed ring part has darker contrast.
On top right & top left there is a butterfly

## Slide 14
-400mV,10pA
Zoffset = 0 to -200 pm
Zoffset = 0 to -200 pm
Butterfly: Voltage dependent df and dI/dV
1.
7 datatsets with 5 different tips.

## Slide 15
Zoffset = 0 to -120 pm
Butterfly: Voltage dependent df and dI/dV
2.
Zoffset = 0 to -120 pm
5 datasets with 3 different tips.

## Slide 16
450 mV
-11.93 ± 0.15 Hz
-12.13 ± 0.15 Hz
1.1 nm
Δdf = 0.20 Hz
Fish: Switching
Distance from atom (nm) | Δdf
1 nm | 0.22 ± 0.3
1.1 nm | 0.20 ± 0.3
1.2 nm | 0.22 ± 0.3
2 datasets with 1 tip

## Slide 17
Coupled atoms: switching
Oscillation OFF
Oscillation ON
Current: 3 states clearly observed
Current: 2 states observed
  AC field of the tip alters (?).
Df: 2 states observed (Δdf ~ 0.3Hz)
2 datasets with 1 tip

## Slide 18: LCPD on different charges
Leo Gross, et al., Science 324 (2009)
charging neutral ⟹ negative
jump to new parabola
Shift in the maxima of parabola
⟹ change in work function
⟹ difference in charge
Possible explanation for dip in LCPD

## Slide 19
Why a dip and not a shift?
Possible explanation for dip in LCPD

## Slide 20
Islands of TAPE on Ag111
Dip feature: charging event at type Q
Seen in other molecules on conducting substrates
N. Kocic et. al. Nano Lett. 15, 4406−4411 (2015)
Carbon 216 (2024); Advanced Material interfaces 7, 15 (2020); J. Appl. Phy. 55,08NAO (2016);
Why a dip and not a shift?
Possible explanation for dip in LCPD

## Slide 21
Possible explanation for dip in LCPD
N. Kocic et. al. Nano Lett. 15, 4406−4411 (2015)
If a rigid shift of force curves: F1 & F2
df remains same, since slope
Except in the area where there is a change.

## Slide 22
Possible explanation for dip in LCPD
N. Kocic et. al. Nano Lett. 15, 4406−4411 (2015)
If a rigid shift of force curves: F1 & F2
df remains same, since slope
Except in the area where there is a change.
Could the dip quantify the charging energy?

## Slide 23: Ideas for further measurement
Can we quantify the dip observed in the df(V) as a charging energy scale: use of df(z) instead?
Is there a shift in LCPD max spatially (with low noise)?
    How does this relate to the screening length and its anisotropy?
    Is this even a parabola?
010
100

## Slide 24: Ideas for further measurement
Can we quantify the dip observed in the df(V) as a charging energy scale: use of df(z) instead?
Is there a shift in LCPD max spatially (with low noise)?
    How does this relate to the screening length and its anisotropy?
    Is this even a parabola?
Anisotropic contrast of charging ring in df:
    Is this reproducible?
    Is this related to the spatial difference in screening?
Df image at +650mV

## Slide 25: Ideas for further measurement
Can we quantify the dip observed in the df(V) as a charging energy scale: use of df(z) instead?
Is there a shift in LCPD max spatially (with low noise)?
    How does this relate to the screening length and its anisotropy?
    Is this even a parabola?
Anisotropic contrast of charging ring in df:
    Is this reproducible?
    Is this related to the spatial difference in screening?
Can we measure an apparent height difference between different states?
    (compensated for electrostatic forces)
    Fish: LCPD first part of the parabola fitted  C.H. df image (Δdf1)
    Mushroom: LCPD first part of the parabola fitted  C.H. df image (Δdf2)
    Coupled atoms (might only work for similar speies)

## Slide 26: Ideas for further measurement
Can we quantify the dip observed in the df(V) as a charging energy scale: use of df(z) instead?
Is there a shift in LCPD max spatially (with low noise)?
    How does this relate to the screening length and its anisotropy?
    Is this even a parabola?
Anisotropic contrast of charging ring in df:
    Is this reproducible?
    Is this related to the spatial difference in screening?
Can we measure an apparent height difference between different states?
    (compensated for electrostatic forces)
    Fish: LCPD first part of the parabola fitted  C.H. df image (Δdf1)
    Mushroom: LCPD first part of the parabola fitted  C.H. df image (Δdf2)
    Coupled atoms (might only work for similar speies)
Is the switching observed differently in df?
    Does the change in df while switching compare with (Δdf1- Δdf2)

## Slide 27: ……..

## Slide 28: Charging event in STS
3d Co state
Charging peak
B. Kiraly, et al., Nat. Comm. 9, 3904 (2018)

## Slide 29: Orbital memory
Co
SUBSTRATE
T. O. Wehling et.al. PRB 84, 235110 (2011)
Fig: ptable.com

## Slide 30
Question 1: Local buckling of BP lattice ?
Charging peak
3d Co state
Image: B. Kiraly
?
Does the BP lattice buckle locally? If so, can we observe/quantify this?

## Slide 31: Orbital memory: Co/BP
Hollow sites
B. Kiraly, et al., Nat. Comm. 9, 3904 (2018)
bi-stable valency
2 different adsorption height
2 different orbital configuration
Configuration stays when electric field is removed.
Local buckling of BP? How to quantify it?
Reversible switching above threshold.

## Slide 32: Spatial anisotropic switching
010
100
Isotropic charging ring.
Anisotropic switching.
Anisotropic charge cloud?
Co: not a point charge?
Possible multipole?
010
100
Inside: charged
Outside: neutral
Spatial extent of charging

## Slide 33: Question 2: What is the spatial distribution of charge on a substrate?
high dielectric
weak hopping
charge localized
Point charge approximation
weak dielectric
more hopping
charge delocalized
Many body problem
e-
e-
e-
e-
e-
e-
e-
SEMICONDUCTOR
INSULATOR
How to measure the charge distribution on the semiconductor?

## Slide 34
Question 3: Adsorption height difference ?
Can we quantify the geometric height using AFM?
3d Co state
e-
e-
e-
e-
e-
e-
SEMICONDUCTOR
If is zero ⟹ chemical contrast dominant
d ?
Possible Polaron?
e-
e-
e-
e-
e-
e-
semiconductor

## Slide 35
Current shows two state switching.
Df within the error margin does nto clearly show.
Amplitude dependent AC field becomes important to consider this.
Might need fine tuning.
Switching at LCPD max voltage is the proof of change in adsorption height but no switching at flat band conditions.
Fish: switching
1.
2.

## Slide 36
450 mV
-11.93 ± 0.13 Hz
-12.15 ± 0.1 Hz
Δdf = 0.22 Hz
-11.93 ± 0.15 Hz
-12.13 ± 0.15 Hz
1 nm
1.1 nm
Δdf = 0.20 Hz
1.2 nm: Δdf = 0.22 Hz
Fish: Switching
Distance from atom (nm) | Δdf
1 nm | 0.22
1.1 nm | 0.22
1.2 nm | 0.22

## Slide 37: Conclusion
dIdV shows charging peak.
LCPD shows dip corresponding to a transiently charged atom.
  Cannot distinguish two LCPD max.
  Is the dip corresponding to a charging energy?
Current shows charging ring isotropic
df shows charging ring as isotropic but contrast within the ring is anisotropic
  Hints to an anisotropic charge distribution in the substrate?

## Slide 38: Local Contact Potential Difference (LCPD)
Vdc
Wilhelm Melitz, et.al., Surface Science Reports, Volume 66, Issue 1 (2011) Noncontact Atomic Force Microscopy (Book)

## Slide 39: Charging event in STS
Inside: charged
Outside: neutral
3d Co state
Charging peak
Spatial extent of charging
B. Kiraly, et al., Nat. Comm. 9, 3904 (2018)
V = 400mV

## Slide 40: Switching moving away from Co
Move in arrow direction, 1 nm, 1.1 nm, 1.2 nm, 1.3 nm
460 mV
-400mV, 150pA

## Slide 41: Switching vs amplitude
30 pm oscillation
70 pm oscillation
-400mV, 150pA
-400mV, 250pA